Weekly report

Lerong Cheng 02/28/2004

In this week, I run process the experiment and figure out the hype-arch trend. The following table shows the hyper arch within delay ranges 9~11ns, 14~16ns, and 19~21ns. It can be seen that in the high performance range (9~11ns), when power gating is applied, vdd will be lower when heterogeneous vt is applied, the same trend will happen, but architecture (N, K) will be similar for all classes. However, in the middle performance range (14~16ns) and the low performance range (19~21ns), applying heterogeneous vt will lead to smaller LUT size and power gating will lead to lower Vt.

| class1 (homogeneous Vt w/o power gating) |  | class2 ( heterogeneous Vt w/o power gating) |
| --- | --- | --- |
| vdd | vt | (N, K) | E (nJ) | D (ns) | ED (nJ.ns) | Area (M) |  | vdd | cvt | ivt | (N, K) | E (nJ) | D (ns) | ED (nJ.ns) | Area (M) |
| 1 | 0.2 | 6,5 | 5.04796 | 9.91105 | 50.0306 | 22.3246 |  | 1 | 0.25 | 0.2 | 10,7 | 4.29179 | 9.92737 | 42.6062 | 23.4742 |
| 1 | 0.2 | 10,5 | 5.14357 | 9.95972 | 51.2285 | 18.0305 |  | 1 | 0.25 | 0.2 | 10,6 | 3.196 | 9.94368 | 31.78 | 23.0011 |
| 0.9 | 0.2 | 6,7 | 4.11083 | 10.4955 | 43.1452 | 35.0517 |  | 1 | 0.25 | 0.2 | 6,6 | 3.21062 | 10.0687 | 32.3267 | 24.8253 |
| 0.9 | 0.2 | 8,7 | 4.23477 | 10.5106 | 44.5097 | 28.649 |  | 1 | 0.2 | 0.25 | 6,7 | 2.14016 | 10.3363 | 22.1213 | 35.0517 |
| 0.9 | 0.2 | 10,6 | 4.20843 | 10.8365 | 45.6045 | 23.0011 |  | 1 | 0.2 | 0.25 | 8,7 | 2.18896 | 10.5566 | 23.108 | 28.649 |
| 0.9 | 0.25 | 10,5 | 1.96685 | 14.1448 | 27.8208 | 18.0305 |  | 0.9 | 0.2 | 0.25 | 6,4 | 0.986026 | 14.0433 | 13.847 | 16.7975 |
| 0.9 | 0.25 | 6,5 | 1.98227 | 14.3551 | 28.4556 | 22.3246 |  | 0.9 | 0.2 | 0.25 | 8,4 | 0.94168 | 14.5406 | 13.6926 | 21.0351 |
| 1 | 0.3 | 8,7 | 1.83072 | 14.5547 | 26.6456 | 28.649 |  | 0.9 | 0.2 | 0.25 | 12,4 | 0.94335 | 14.8063 | 13.9675 | 16.1356 |
| 1 | 0.3 | 6,7 | 1.81915 | 14.9984 | 27.2844 | 35.0517 |  | 0.9 | 0.2 | 0.25 | 10,4 | 0.931658 | 14.927 | 13.9068 | 17.1804 |
| 1 | 0.3 | 10,6 | 1.73831 | 15.0157 | 26.1019 | 23.0011 |  | 0.9 | 0.3 | 0.25 | 12,4 | 0.910545 | 17.1592 | 15.6242 | 16.1356 |
| 0.9 | 0.3 | 6,6 | 1.33199 | 18.6468 | 24.8374 | 24.8253 |  | 0.9 | 0.2 | 0.3 | 12,4 | 0.844421 | 18.8659 | 15.9308 | 16.1356 |
| 0.9 | 0.3 | 8,5 | 1.27607 | 19.3733 | 24.7216 | 22.9694 |  | 0.9 | 0.2 | 0.3 | 10,4 | 0.831543 | 18.9012 | 15.7172 | 17.1804 |
| 0.9 | 0.3 | 10,5 | 1.26568 | 19.7914 | 25.0495 | 18.0305 |  | 0.9 | 0.25 | 0.3 | 6,4 | 0.82173 | 19.0375 | 15.6437 | 16.7975 |
| 0.9 | 0.3 | 12,4 | 1.18855 | 21.2367 | 25.2408 | 16.1356 |  | 0.9 | 0.25 | 0.3 | 12,4 | 0.76603 | 19.3009 | 14.785 | 16.1356 |
| 0.9 | 0.3 | 6,4 | 1.23021 | 21.567 | 26.5318 | 16.7975 |  | 0.9 | 0.25 | 0.3 | 8,4 | 0.781245 | 19.761 | 15.4382 | 21.0351 |
| class3 (homogeneous Vt w/ power gating) |  | class4 (heterogeneous Vt w/ power gating) |
| vdd | vt | (N, K) | E (nJ) | D (ns) | ED (nJ.ns) | Area (M) |  | vdd | cvt | ivt | (N, K) | E (nJ) | D (ns) | ED (nJ.ns) | Area (M) |
| 1 | 0.2 | 6,6 | 3.21739 | 9.93166 | 31.954 | 30.5057 |  | 1.1 | 0.2 | 0.25 | 10,7 | 8.3039 | 9.92247 | 82.3952 | 32.608 |
| 1 | 0.2 | 10,6 | 3.13763 | 9.95829 | 31.2454 | 28.9013 |  | 1.1 | 0.2 | 0.25 | 6,6 | 5.52215 | 9.9374 | 54.8758 | 30.5057 |
| 1 | 0.2 | 8,6 | 3.05611 | 10.2348 | 31.2788 | 27.8861 |  | 1.1 | 0.2 | 0.25 | 10,6 | 5.55506 | 10.0034 | 55.5695 | 28.9013 |
| 1 | 0.2 | 8,5 | 2.83843 | 10.4217 | 29.5812 | 28.332 |  | 1.1 | 0.2 | 0.25 | 8,6 | 5.60704 | 10.187 | 57.1189 | 27.8861 |
| 1 | 0.2 | 6,5 | 2.83243 | 10.5321 | 29.8314 | 27.2525 |  | 1.1 | 0.2 | 0.25 | 8,5 | 3.7206 | 10.3616 | 38.5515 | 28.332 |
| 0.9 | 0.25 | 6,6 | 1.33373 | 13.8835 | 18.5168 | 30.5057 |  | 0.9 | 0.2 | 0.25 | 6,4 | 0.759699 | 13.9468 | 10.5954 | 21.3935 |
| 0.9 | 0.25 | 8,6 | 1.26143 | 14.3439 | 18.0939 | 27.8861 |  | 0.9 | 0.2 | 0.25 | 8,4 | 0.720809 | 14.4748 | 10.4336 | 25.5521 |
| 0.9 | 0.25 | 8,5 | 1.24709 | 14.5357 | 18.1273 | 28.332 |  | 0.9 | 0.2 | 0.25 | 12,4 | 0.71221 | 14.7575 | 10.5104 | 21.1519 |
| 0.9 | 0.25 | 10,5 | 1.18571 | 14.7848 | 17.5304 | 23.4103 |  | 0.9 | 0.2 | 0.25 | 10,4 | 0.713158 | 14.916 | 10.6374 | 21.688 |
| 0.9 | 0.25 | 12,4 | 1.10094 | 15.9858 | 17.5994 | 21.1519 |  | 0.9 | 0.2 | 0.3 | 6,4 | 0.696488 | 16.5263 | 11.5104 | 21.3935 |
| 1 | 0.3 | 10,4 | 0.990124 | 18.4763 | 18.2938 | 21.688 |  | 0.9 | 0.2 | 0.3 | 10,4 | 0.646606 | 17.7106 | 11.4518 | 21.688 |
| 0.9 | 0.3 | 6,6, | 0.982521 | 19.0062 | 18.674 | 30.5057 |  | 0.9 | 0.25 | 0.3 | 12,4 | 0.63274 | 18.8581 | 11.9323 | 21.1519 |
| 0.9 | 0.3 | 8,6 | 0.940007 | 19.7145 | 18.5317 | 27.8861 |  | 0.8 | 0.2 | 0.3 | 8,5 | 0.607942 | 20.7055 | 12.5877 | 28.332 |
| 0.9 | 0.3 | 8,5 | 0.920827 | 19.8029 | 18.235 | 28.332 |  | 0.8 | 0.2 | 0.3 | 6,4 | 0.56899 | 21.1492 | 12.0337 | 21.3935 |
| 0.9 | 0.3 | 10,5 | 0.889114 | 20.2149 | 17.9734 | 23.4103 |  | 0.8 | 0.2 | 0.3 | 8,4 | 0.537595 | 22.0082 | 11.8315 | 25.5521 |